IOE

IOE

# Upcycled Debris Block

ढुङ्गा/ईटा मिस्रित बलियो ब्लक

# as Construction Material

# Introduction

April 25 Gorkha earthquake resulted in complete collapse of about 5,00,000 buildings posing enormous challenges in debris management and material transportation for reconstruction in rural areas.

The overarching objective of the research was to develop an Upcycled Debris Block that could be used for the reconstruction of the collapsed buildings at affordable price especially in rural areas.

Theory of Compressed Soil Earthen Block has been adopted for Upcycled Debris Block (Dhunga wa Etta Misrit Baliyo Block) using the debris from the collapsed buildings along with different combination of sand and cement. The blocks are designed, developed and tested in Lab of Pulchowk Engineering Campus and results are tabulated and analysed.

# Tools Used

Simple tools, easily available in the rural context, like shovel, hammer are used. An iron mould of inner dimension 12"X8"X6" along with a hard wood rammer of 30"X3"X3" was made on site.

# Materials used

Debris from collapsed building (Brick/ Stone masonry with mud mortar)

Sand       		Cement

Water     		Soil for mortar

# Process

The process starts with segregation of Debris into rubbles, soil and whole brick/ stone. The whole brick/ stone can directly be used as construction material while the broken bricks and rubbles are segregated.  The soil is beaten to dust and kept separately. Other materials like sand/ gravel and cement is purchased from market.

## Mix for block

Realizing the rural context, three block mix have been adopted i.e. 1:2:4, 1:3:6, 1:4:8. It shows that the block will have about, 15%, 10% or 7.5% of cement by volume. Coarse sand/ gravel is also mixed to make soil well graded as soil from debris is mostly clay.

Segregated stone/ brick and rubbles/ pebbles are mixed thoroughly with soil, sand and cement in proper proportion as per the mix design with water cement ratio of 0.5 to 0.7. A minimum amount of water is applied so that the mix is just wet which does not stick to hand.

## Preparation of Mould

The iron mould is painted with used Mobil or any other oil so that unmoulding becomes easy. The mould is filled with the mix in layers and rammed with the hard wooden rammer (30"X3"X3"). In each layer the mould is rammed at least 50 to 60 times to achieve optimum density. No void should be left.

## Unmoulding

Once the compaction is achieved, the mould is unmoulded carefully and the block is ready. However, the block needs to be left at the same place for next 24 hrs and then could be handled.

## Curing

Curing should start only after 48 hrs to 72 hrs. Two techniques of curing have been applied. In the first case the conventional technique of covering the blocks with jute and sprinkling water thrice a day i.e. at 9 am, 12 am and 3 pm. The other technique is to wrap all the blocks in plastic. It does not require any further water. The moisture from the block itself will cure the block.

## Testing

The compressive strength of each type of block has been tested after 7 days, 14 days and 28 days.

However, the initial test showed that blocks do not gain much strength in 7 days but handling could be done. Therefore, the 7 days’ tests are discarded and only 14 days’ and 28 days’ tests were carried out.

# Process of Preparation of the Upcycled Debris Block

## Types and Number of Blocks Tested

3 types of mixes are designed. For each mix 8 blocks were tested for 14 and 28 days respectively for jute covered water sprinkling curing method. Similarly, for plastic wrapped curing, 3 blocks were tested for 14 days and 28 days. Total number of block tested is 132.

# Test Results

The test results of both Stone Debris Blocks and Brick Debris Blocks show that the compressive strength of these blocks is comparable with compressed stabilized earthen block. If it is compared with the strength of adobe construction, it is well above. The strength could be further increased if good soil (Gravel= 15%, Sand = 50%, Silt = 15% and Clay = 20%) is used. The average proportion of cement stabilizer is about 10%.

# Cost of Production

The cost of production of each block is about 80 to 100 NRS, which is similar to brick in the market. The price of production will considerably go down to 60% with commercial production and more number of moulds.

# Advantages

Debris Management	Cost Effectiveness	Energy Effectiveness

Technology Transfer	Biodegradable		Local Economy

Low imports		Green recovery and Reconstruction

# Uses

Reconstruction of houses in rural areas

# Developed in Collaboration with

Centre for Disaster Studies (CDS), Institute of Engineering(IOE)

Phone #: +977 (01) 5530769 | Email: cds@ioe.edu.np; ajay.cord@gmail.com

# Supported by

Comprehensive Disaster Risk Management Programme (CDRMP), UNDP Nepal